## Slide 1: 226Ra for the production of 227Ac, 228Th and useful decay daughters
Dan Stracener
Oak Ridge National Laboratory
Workshop on
Radioactive Isotopes for Fundamental Physics
August 25 – 27, 2026
This work is supported by the Office of Isotope R&D and Production in the U.S. Department of Energy.

## Slide 2: Radium – the original radioisotope for medical use
Radium was discovered by Marie and Pierre Curie in 1898 (a few months after they discovered polonium) and in 1907 determined the mass to be 226.45 amu
Marie Curie won the Nobel Prize in Chemistry 1911 for these discoveries
By 1901, 226Ra was being used to treat skin lesions
The Curie as a unit of radioactivity was defined in 1910 as the activity emanating from 1 gram of 226Ra and was named in honor of Pierre Curie
  Marie Curie accepted this definition after she insisted that 1 Curie should correspond to 1 gram of 226Ra rather than 10 ng as was originally proposed
Brachytherapy is a type of radiation therapy where a sealed radioactive source is placed into or near a tumor.
226Ra devices were used to treat various cancers from the 1920 to 1960s.
226Ra use was discontinued by the late 1960s.

## Slide 3: Recovery from Legacy Radium Medical Devices
Plaques
Tubes
Needles
Individual sources contain various amounts of 226Ra
Devices are mechanically disassembled, and radium is chemically dissolved from the fragments
Notes: Sources-Plaques not viable, solids filler material makes difficult
Smaller needles and tubes are preferable-easier to mechanically open

## Slide 4: Examples of legacy medical devices containing 226Ra
Legacy 226Ra devices received at ORNL from repositories around the world
These legacy medical devices come in a large variety of shapes and sizes
Variety of needles, tubes and cylinders in the SFC
Glass ampoule
Plaque

## Slide 5: More examples of legacy medical devices containing 226Ra

## Slide 6: Dissolving and purifying 226Ra
The chemistry to purify the 226Ra material is not trivial
The ‘filler’ material is quite varied, including
  Group 2 elements (Ca, Ba, …)
  Transition metals (Cu, Ni, Ag, …)
  Pb and Bi
  Pt and Ir from the devices
The process must be versatile and optimized to reduce the volume of waste generated

## Slide 7: 226Ra is important for the DOE Isotope Program
A valuable feedstock for production of alpha-emitting radioisotopes at HFIR
ORNL is uniquely qualified for large scale processing and irradiation of 226Ra targets
  HFIR, infrastructure (hot cells, gloveboxes, transportation), safety systems, radiochemistry experience
S. Hogle et al., Reactor Production of Thorium-229, Appl. Radiat. Isot. 114, 19 (2016)

## Slide 8: Hydraulic Tube at the 85 MW High Flux Isotope Reactor
The HFIR hydraulic tube facility allows for targets to be inserted/removed during operation of the reactor
This makes it possible to optimize production of isotopes, such as 227Ac and 228Th (while minimizing unwanted radioisotopes that contribute to radioactive waste)

## Slide 9: Fabricating 226Ra targets for HFIR irradiation
Purified 226Ra is pressed into solid pellets for irradiation at HFIR
  Mixture of RaCO3 and aluminum powder (for thermal conductivity)
Heat is generated in the target during irradiation, and it must be removed efficiently to prevent melting
  Heat capacity, thermal conductivity, and thermal expansion are all considered in the heat calculations that are required to determine target temperature during irradiation at HFIR
Preparation of 226Ra targets in a glovebox

## Slide 10: Reducing environmental emissions with in-cell controls
Schematic of in-cell gas trapping apparatus
Evaporation set-up in the hot cell with heat lamp and venturi collector that is connected to the HOG system

## Slide 11: Storing 226Ra
Purified 226Ra is stored in the hot cell in a low-molarity nitric acid solution in a borosilicate glass flask until needed
For R&D shipments, aliquots of this solution are dispensed into either glass vials or Zircaloy vials and evaporated to dryness as solid radium nitrate
226Ra dissolved in low-molarity nitric acid
Prior to target fabrication, 226Ra is purified to a strict material specification, including
  >99% radionuclidic purity
  limits on ‘cold’ element contamination

## Slide 12: 226Ra decay chain
90
89
88
87
86
85
84
83
82
81
80
124 126 128 130 132 134 136 138 140
226Ra (T½ = 1600 y)
5 a-decays
4 b-decays
Long-lived daughters
  222Rn (T½ = 3.8 d)
  210Pb (T½ = 22.2 y)
  210Bi (T½ = 5.0 d)
  210Po (T½ = 138.4 d)
terminates in 206Pb

## Slide 13: 227Ac decay chain
90
89
88
87
86
85
84
83
82
81
80
124 126 128 130 132 134 136 138 140
227Ac (T½ = 21.77 y)
5 a-decays
3 b-decays
Long-lived daughters
  227Th (T½ = 18.7 d)
  223Ra (T½ = 11.4 d)
terminates in 207Pb

## Slide 14: 228Th decay chain
90
89
88
87
86
85
84
83
82
81
80
124 126 128 130 132 134 136 138 140
228Th (T½ = 1.91 y)
5 a-decays
2 b-decays
Long-lived daughters
  224Ra (T½ = 3.63 d)
terminates in 208Pb

## Slide 15: Medical uses for these alpha-emitters
227Ac (t1/2 = 21.7 a) is the parent isotope of 223Ra (t1/2 = 11.4 d) the active pharmaceutical ingredient in Xofigo®
  Provides both prolonged survival and palliative effects
Xofigo (223Ra dichloride) is approved worldwide for the treatment of castration-resistant prostate cancer with bone metastases
228Th (t1/2 = 1.91 a) is the parent isotope of 224Ra (t1/2 = 3.6 d) which then decays to 212Pb and 212Bi
212Pb is being studied in several clinical trials to treat neuroendocrine tumors solid tumor via targeted alpha therapy
212Pb can also be used in conjunction with 203Pb as an imaging agent to create a theranostic pair
224Ra is being studied for direct use in several cancer types that have metastasized to the bone
These clinical trials are very encouraging and subsequently, the demand for 228Th is increasing exponentially
229Th (t1/2 = 7920 y) can also be produced via irradiation of 226Ra targets in HFIR
This long-lived isotope decays by a-emission to 225Ac (t1/2 = 9.9 d)
Clinical trails with 225Ac are in progress to treat solid and blood tumors via targeted alpha therapy techniques
Another decay daughter of 227Ac is being used in an application called TTC (targeted thorium conjugates)
227Th (t1/2 = 18.7 d) is being studied for treatment of solid and blood tumors (e.g., ovarian, breast, prostate, colorectal, …)

## Slide 16: Recent chemistry publications with 226Ra
F.D. White, N.A. Thiele, M.E. Simms, and S.K. Cary, Structure and bonding of a radium coordination compound in the solid state. Nature Chemistry 16, 168–172 (2024).
A.S. Ivanov, M.E. Simms, V.S. Bryantsev, P.D. Benny, J.R. Griswold, L.H. Delmau, and N.A. Thiele, Elucidating the Coordination Chemistry of the Radium Ion for Targeted Alpha Therapy. Chemical Communications 58, 9938-9941 (2022).
From a DOE Office of Science Highlight, illustrating the 11-coordinate structure of radium (different from the 10-coordinate structure observed for barium).
“… results emphasize the disparate coordination chemistries of Ra2+ and Ba2+, such that using Ba2+ as a non-radioactive surrogate to model the behaviour of Ra2+ in studies must be done with caution.”
Ba and Ra single crystal structures prepared with the DB30C10 ether macrocycle

## Slide 17: Recent publications on laser spectroscopy of 226Ra
S.M. Udrescu, et al., Precision spectroscopy and laser-cooling scheme of a radium-containing molecule. Nat. Phys. 20, 202–207 (2024).
“… high-resolution laser spectroscopy of radium monohydroxide, monodeuteroxide, and monofluoride molecules (226RaOH, 226RaOD, and 226RaF) in a tabletop apparatus by combining trace radioactive target production protocols, optically driven chemistry in a cryogenic buffer gas, and low-background spectroscopic detection methods.”
C.J. Conn, et al., Production and spectroscopy of cold radioactive molecules. Science 393, 319-323 (2026).
“… nuclear octupole deformation of certain radium isotopes massively boosts the sensitivity of radium monofluoride molecules to symmetry-violating nuclear properties.”
“… measurements of the rovibronic structure of radium monofluoride molecules, which allow the determination of their laser cooling scheme.”

## Slide 18: Thanks for your attention
Cherenkov radiation from dispensed 226Ra in glass vials (1 mCi each)